Izrada proizvoda od kompozita

4.1 Osnove izrade proizvoda od kompozita 2 4.1.1 Komponente i karakteristike kompozita 2 4.1.2 Oblikovanje proizvoda od kompozita 7 4.1.3 Postupci oblikovanja proizvoda od kompozita 7 4.1.4 Materijali koji se koriste u izradi proizvoda od kompozita 8 4.2 Postupci izrade proizvoda s polimernom matricom 8 4.2.1 Pultruzija 8 4.2.2 Laminiranje 8 4.2.3 Prešanje 8 4.2.4 Centrifugalno kalupljenje 8 4.3 Postupci izrade proizvoda s keramičkom matricom 18 4.3.1 Toplo prešanje 18 4.3.2 Toplo izostatičko prešanje HIP (en. Hot Isostatic Pressing) 18 4.3.3 Sinteriranje iz tekuće faze 18 4.4 Postupci izrade proizvoda s metalnom matricom 19 4.4.1 Lijevanje s miješanjem 19 4.4.2 Infiltracija 19 4.4.3 Depozicija 19 4.4.4 Difuzijsko spajanje 19 4.4.5 Formiranje s deformacijom 19 4.5 Procesi izrade i proizvodi od kompozita 22 4.5.1 Granične površine faza 22 4.5.2 Mehanička svojstva kompozita 22 4.5.3 Usporedba postupaka 22 4.5.4 Greške i njihovo otklanjanje 22 Literatura 22

Kompoziti – višefazni materijali s jasno izraženim granicama faza, kod kojih dva više materijala različitih kemijskih sastava (metali, keramike, polimeri) i/ili oblika (zrna, vlakna, lamele) formiraju jedinstvenu strukturu s jasno izraženim granicama. Kombiniranjem komponenata kompozita postižu se specifične kombinacije svojstava (čvrstoća, gustoća, krutost, tvrdoća, toplinska i električna vodljivost). Svojstva kompozita ovise o svojstvima komponenata, njihovim kemijskim i konstitucijskim sastavima.

Faze su uniformni dijelovi kompozita, a komponente različite tvari koje sadrži kompozit.

Za izradu niza dijelova/sustava – S-5.1 (industrije vozila, zrakoplova, sportske opreme, opreme za kućanstva, brodogradnja, vodoopskrba, sanacija otpadnih voda) kompoziti mogu zamijeniti najčešće korištene metale – željezo i aluminij, pri čemu se često postižu bolje performanse dijelova/sustava. Na primjer, s kompozitima se postiže manja masa, u slučaju zamjene čelika za 60 ÷ 80 %, u slučaju zamjene aluminija 20 ÷ 50 %.

Slika S-5.1  Proizvodi od kompozita

## Osnove izrade proizvoda od kompozita

Prema tome, izrada proizvoda od dvokomponentnog kompozita može se prikazati općom blok shemom:

Slika S-5.2  Blok shema izrade proizvoda od kompozita

### Komponente i karakteristike kompozita

Dvije su osnovne konstitucijske komponente kompozita:

|  | matrica – osnovni materijal određenih svojstava dodatak – materijal čijim se dodavanjem postižu potrebne kombinacije svojstava kompozita |
| --- | --- |

Kod kompozita se često koriste kratice:

- kompoziti s metalnom matricom – MMC (en. Metal Matrix Composites)

- kompoziti s keramičkom matricom – CMC (en. Ceramic Matrix Composites)

- kompoziti s polimernom matricom – PMC (en. Polymer Matrix Composites)

Kompoziti se mogu sistematizirati prema matrici i prema dodatku više načina:

| prema matrici | prema dodatku |
| --- | --- |

In the structural composites category, laminates are the one in which layers are stacked and subsequently cemented together such that the orientation of the high-strength directions varies with each successive layer. Sandwich panels consists of two strong outer sheets, separated by a layer of less-dense material (core), which has lower stiffness and lower strength.

Najviše se koriste kompoziti s duromernom (polimernom) matricom, a još širu primjenu im ograničavaju poteškoće uz automatizaciju proizvodnje dijelova. Razvoj tehnologije oblikovanja prahova potiče šire korištenje kompozita s metalnom matricom. Primjena kompozita s keramičkom matricom najmanje je raširena.

Primjeri su često korištenih kompozita:

- s dodatkom velikih čestica – beton, smjesa cementa i šljunak (keramička matrica i keramički dodatak);

- s dodatkom dugim vlaknima – staklom ojačana plastika, smjesa EP smole i staklenih vlakana (polimerna matrica i keramički dodatak);

- strukturni slojeviti – "šperploča", izmjenični slojevi: (a) tanka ploča od drveta (smjer vlakana susjednih slojeva je u pravilu 90° ili 45°), (b) ljepilo za drvo (polimer).

Svojstva kompozita ovise o komponentama (matrica/dodatak), njihovim:

svojstvima,

udjelima,

oblicima, veličinama i raspodjelama,

prirodama i jakostima uzajamnih veza.

Karakteristike su kompozita u velikoj mjeri različite.

| Materijal | matrica | Titan | Ugljik | Poliester | Epoksid |
| --- | --- | --- | --- | --- | --- |
|  | dodatak | titan-karbid čestice | ugljična vlakna | stakleno tkanje | stakleno tkanje | aramidno tkanje | ugljično tkanje |
| Sastav, wi % | 20 TiC(p) | 50 C(Vf) | tvorničko tkanje | tkanje (kil) | tkanje (kil) | tkanje (kil) |
| (, kg/dm3 | 4,52(4,58 | 1,68(1,72 | 1,6(2,0 | 1,75(1,97 | 1,38 | 1,54(1,61 |
| Rm, N/mm2 | 950(1040 | 220(250 | 175(345 | 31,9(35,1 | 92(106 | 470(668 |
| Rm,t, N/mm2 | 960(1050 | 14(23 | 210(350 | 319(351 | 129(152 | 450(649 |
| E, kN/mm2 | 140(160 | 90(100 | 14(31 | 66,3(69,7 | 24(31 | 44(48 |
| (, – | 0,33(0,35 | 0,31(0,33 | 0,30(0,35 | 0,31(0,32 | 0,33(0,35 | 0,33(0,34 |
| Re, N/mm2 | 940(1040 | 14(23 | 166(276 | 207(304 | 129(152 | 450(649 |
| A, % | 0,3÷0,31 | 0 | 1÷2 | 0,85÷0,95 | 0,37÷0,42 | 0,84÷0,93 |
| KIC, N/m3/2 | 580(890 | 180(200 | 340(660 | 190(950 | 190(1400 | 190(2800 |
| HV | 240(270 | 67(74 | 50(83 | 11(22 | 11(22 | 11(22 |
| Rd,is, N/mm2 | 26,9(31,3 | 15(17 | 83(138 | 41(91 | 71(99 | 247(477 |
| tMax, °C | 380(430 | 2000(2100 | 170(190 | 140(220 | 140(220 | 140(220 |
| tmin, °C | –273 | –273 | –120÷–70 | –120÷–70 | –120÷–70 | –120÷–70 |
| c, J/(kg◦K) | 585(590 | 754(758 | 1150(1210 | 1020(1120 | 510(690 | 950(1090 |
| (, W/(m◦K) | 5,5(6,0 | 10(70 | 0,65(0,68 | 0,42(0,51 | 0,19(0,26 | 1,1(2,2 |
| (, (m/(m◦K) | 7,7(8,4 | 0,6(8,2 | 27(54 | 8,6(33 | 9,4(13 | 5,5(29 |
| Ek, MV/m | – | 10(20 | 14(20 | 12(20 | 12(20 | – |
| e0, ((◦cm | 180(190 | 1100(2700 | 1018(1019 | 2◦1021(2◦1022 | 3◦1019(2◦1021 | 2◦105(7◦105 |
| krecikličnosti | 0 | 0 | 0,015 | 0,015 | 0,015 | 0,015 |
| Cijena, kn | 600(850 | 60(85 | 58(66 | 70(156 | 910(990 | 470(550 |
| Otpornost na: |  |  |  |  |  |  |
| trošenje | dobra | dobra | srednja | srednja | srednja | srednja |
| oksidaciju (500°C) | vrlo dobra | slaba | vrlo slaba | vrlo slaba | vrlo slaba | vrlo slaba |
| paljenje | vrlo dobra | srednja | slaba | dobra | dobra | dobra |
| UV zrake | vrlo dobra | vrlo dobra | vrlo dobra | dobra | dobra | dobra |
| slatku vodu | vrlo dobra | vrlo dobra | vrlo dobra | vrlo dobra | vrlo dobra | vrlo dobra |
| morsku vodu | vrlo dobra | vrlo dobra | vrlo dobra | vrlo dobra | dobra | vrlo dobra |
| jake kiseline | dobra | dobra | srednja | srednja | srednja | srednja |
| jake lužine | dobra | slaba | srednja | vrlo dobra | vrlo dobra | vrlo dobra |
| slabe kiseline | vrlo dobra | vrlo dobra | vrlo dobra | vrlo dobra | vrlo dobra | vrlo dobra |
| slabe lužine | vrlo dobra | vrlo dobra | srednja | vrlo dobra | vrlo dobra | vrlo dobra |
| organska otapala | vrlo dobra | vrlo dobra | srednja | dobra | dobra | dobra |
| Materijal | matrica | Titan | Ugljik | Poliester | Epoksid |
|  | dodatak | titan-karbid čestice | ugljična vlakna | stakleno tkanje | stakleno tkanje | aramidno tkanje | ugljično tkanje |

EMERGING CLASSES of composites:	Hybrid Composites

Functionally Graded Composites

Nano Composites

Hybrid Composites use two or more different kinds of fibers in a single matrix. Example- carbon and glass fibers incorporated into a polymeric matrix. This glass-carbon hybrid is stronger, tougher and has higher impact resistance. The failure of hybrid composites is non-catastrophic. Carbon fibers are first to fail and the load is transferred to glass fibers. Upon failure of glass fibers, the matrix phase sustains the applied load till the composite fails.

Functionally Graded Composites are engineered by spatially varying the microstructural details through non-uniform distribution of reinforcement phase, by using reinforcement with different properties/ sizes or shapes. The result is a composite that produces continuously changing thermal and mechanical properties at a macroscopic level.

Nano Composites uses nanoparticles/ carbon nanotubes as an alternative material to dispersed phase in composites. Single-walled carbon nanotubes (SWNTs) possess a unique combination of high strength, high modulus, and high elongation. 40 percent increase in flexure strength of a structural epoxy with the addition of 10 weight percent SWNTs has been demonstrated

#### Primjeri proizvoda i postupaka

Elektrotehnika:

električna izolacija dijelova, izolacija od utjecaja elektromagnetnih valova, podloge sklopki, podloge tiskanih kola, oklopi, kućišta, poklopci, satelitske antene, radarske antene, kupole, vrhovi TV tornjeva, kanali za kablove, vjetrenjače

Građevinarstvo:

stambene jedinice, dimnjaci, betonske konstrukcije, različiti pokrovi (kupole, prozori), bazeni za plivanje, pročelja zgrada, profili, unutarnji zidovi, vrata, namještaj, kupaone, telefonske kabine

Transport cestama:

dijelovi karoserije, kompletne karoserije, volani, branici, rešetke hladnjaka, vratila transmisije, opruge ogibljenja, spremnici za plin, šasije, zglobovi ogibljenja, navlake, kabine, sjedišta, autocisterne, hladnjače, prikolice

Transport željeznicom:

čeoni dijelovi lokomotiva, konstrukcijski dijelovi vagoni, vrata, sjedišta i unutarnje pregrade putničkih vagona, kućišta ventilatora, kabine žičara

Transport morem:

brodovi lebdjelice (hoverkrafti), brodovi za spašavanje, patrolni brodovi, male ribarice, ribarski brodovi, oprema za iskrcaj, minolovci, regatne brodice, brodice za zabavu, kanui

Zračni transport:

konstrukcijski dijelovi putničkih zrakoplova, jedrilice, kupole, usmjerivači zraka, krilca, vertikalni stabilizatori, krakovi elise helikoptera, propeleri, vratila transmisije, diskovi kočnica zrakoplova, svemirske letjelice

Application of advanced composite materials in Boeing 757-200 commercial aircraft.

Svemirski transport:

startne rakete, spremnici, sapnice, oplate za ulazak u atmosferu

Opće strojarstvo:

zupčanici, ležajevi, zaštitni pokrovi, tijela dizalica, ruke robota, naplatci, letve za tkanje, cijevi, dijelovi ploče za crtanje, boce za komprimirani plin, cijevi za morske platforme, radijalni pneumatici

Sport i rekreacija:

reketi za tenis i skvoš, štapovi za pecanje, skije, štapovi za skok preko motke, jedrilice, daske za jedrenje, daske za surfanje, daske za koturanje, lukovi i strijele, atletska koplja, zaštitne kacige, okvir bicikla, oprema za golf, oprema za sportsko veslanje

#### Prednosti i nedostaci

Proizvodi, Postupci

Advantages 
of using Composites

- For the same strength, composites are lighter than steel by 80% and aluminum by 60%.

- Tailorable thermal expansion properties (can be compounded to closely match surrounding structures to minimize thermal stresses)

- Exceptional formability (can be formed into many complex shapes during fabrication)

- Low observablity (can be seeded with appropriate materials to absorb electromagnetic waves)

### Oblikovanje proizvoda od kompozita

Oblikovanje proizvoda

### Postupci oblikovanja proizvoda od kompozita

Klasifikacija postupaka

For Polymer Matrix Composites

    - Pultrusion

    - Filament winding

    - Resin Transfer Molding (RTM)

    - Vacuum Assisted Resin Transfer Molding (VARTM)

    - Hand Layup of prepeg

For Ceramic Matrix Composites

    - Hot Pressing

    - Hot Isostatic Pressing (HIP)

    - Liquid Phase Sintering

For Metal Matrix Composites

    - Stir Casting

    - Squeeze Infiltration

    - Reactive Processing

    - Powder Blending & Consolidation

    - Physical Vapor Deposition

    - Particle-Liquid Sheet Impingement Technique

    - Two stage process: Quick-Set and Quick- Cast

### Materijali koji se koriste u izradi proizvoda od kompozita

## Postupci izrade proizvoda s polimernom matricom

Postupci su izrade proizvoda s polimernom matricom:

### Pultruzija

### Laminiranje

### Prešanje

### Centrifugalno kalupljenje

- Vacuum Assisted Resin Transfer Molding (VARTM)

- Hand Layup of prepeg

- Pultrusion

Continuous fiber rovings are first impregnated with a thermosetting resign, these are then pulled through a steel die which preforms the desired shape  and also establishes the resign/ fiber ratio. The stock then passes through curing die which is imparts the final shape; this die is also heated in order to initiate curing of the resign matrix. A pulling device draws the stock through the dies.

Tubes and hollow sections can be made possible by using central mandrels or  inserted hollow cores. Pultrusion is used for manufacturing of components having continuous lengths and a constant cross sectional shape. Principle reinforcements are glass, carbon and aramid fibers, normally added in concentrations between 40 and 70 vol%. Commonly used matrix materials include polyesters, vinyl esters and epoxy resins.

- Filament winding

Filament winding is a process by which continuous reinforcing fibers are accurately positioned in a predetermined pattern to form a hollow (usually cylindrical) shape. The fibers are fed through a resign bath and then continuously wound onto a mandrel. After appropriate number of layers have been applied , curing is carried out after which mandrel is removed

Filament wound parts have very high strength to weight ratios. Common filament wound defence application is rocket motor casing. Various winding pattern are possible (i.e. circumferential, helical etc.) to give desired mechanical characteristics.

- Resin Transfer Molding (RTM)

RTM is commonly referred to a ‘closed mold process’ in which reinforcement material is placed between two matching mold surfaces- bottom mold and top mold the mold set is then closed and clamped and a low viscosity thermoset resin is injected under moderate pressures (50-100 psi) into the mold cavity through a port or a series of ports within the mold. The resign thus wets out all surfaces of reinforcements. The part is then cured under heat and pressure.

This process can produce parts faster- as much as 5-20 times faster than open molding techniques. RTM produces tighter dimensional tolerances to within 
+ 0.005 inch. Complex mold shapes can be achieved and mold surface can produce a high quality finish.

- (VARTM)

This process use the injection of resign in combination with a vacuum. Parts using VARTM are made by placing dry reinforcing fabrics into a mold, applying a vacuum bag to the open surface and pulling the vacuum while at the same time infusing a resin to saturate the fibers until the part is fully cured. Heat and pressure are applied for curing. A vacuum is applied to the bag to remove air and volatile products.

- Hand Layup of prepeg

Prepregging involves the application of formulated resin products, in solution or molten form, to a reinforcement such as carbon, fiberglass or aramid fiber or cloth. The prepreg product is trimmed and laid down over a mold where it is formed to the desired shape. Several layers may be required. After forming, a vacuum bag is sealed around the lay-up.  Vacuum is pulled on the raw prepreg to remove air and compact the part. Then the assembly is placed in an autoclave for cure under heat and pressure.

Most parts made by hand lay-up or automated tape lay-up must be cured by a combination of heat, pressure, vacuum, and inert atmosphere. To achieve proper cure, the part is placed into a plastic bag inside an autoclave. A vacuum is applied to the bag to remove air and volatile products. Heat and pressure are applied for curing. Usually an inert atmosphere is provided inside the autoclave through the introduction of nitrogen or carbon dioxide.

This autoclave can achieve temperatures up to 350 degrees F and pressures up to 105 pounds per square inch. The autoclave has a working size of: 8 feet in diameter and up to 26 feet in length. A computer controls the entire process, and an accurate record is kept of the entire curing process.

Schematic illustration of methods of reinforcing plastics (matrix) with (a) particles, (b) short or long fibers or flakes, and (c) continuous fibers.  The laminate structures shown in (d) can be produced from layers of continuous fibers or sandwich structures using a foam or honeycomb core

Specific tensile strength (tensile strength-to-density ratio) and specific tensile modulus (modulus of elasticity-to-density ratio) for various fibers used in reinforced plastics.  Note the wide range of specific strengths and stiffnesses available.

Cross-section of a tennis racket, showing graphite and aramid (Kevlar) reinforcing fibers.  Source:  Courtesy of J. Dvorak, Mercury Marine Corporation and F. Garret, Wilson Sporting Goods Co. (b)  Cross-section of boron fiber-reinforced composite material

The effect of type of fiber on various properties of fiber-reinforced nylon

(a)  Fracture surface of a glass fiber-reinforced epoxy composite.  The fibers are 10μm (400μin.) in diameter and have random orientation.  (b)  Fracture surface of a graphite fiber-reinforced epoxy composite.  The fibers, 9 μm to 11μm in diameter, are in bundles and are all aligned in the same direction.

The tensile strength of glass-reinforced polyester as a function of fiber content and fiber direction in the matrix.

Cross-section of a composite sailboard, an example of advanced materials construction. Source: K. Easterline, Tomorrow’s Materials (2nd ed.), p. 133.  Institute of Metals, 1990.

Examples of metal-matrix composite parts.  Source:  Courtesy of Metal Matrix Cast Composites, LLC.

Tapes used in Making Reinforced Plastic Parts

Manufacturing process for polymer-matrix composite tape.  (b)  Boron-epoxy prepreg tape.  These tapes are then used in making reinforced plastic parts and components with high strength-to-weight ratios, particularly important for aircraft and aerospace applications and sports equipment.  Source:  (a)  Courtesy of T. W. Chou, R. L. McCullough, and R. B. Pipes. (b)  Courtesy of Avco Specialty Materials/Textron.

Tape and Tape-Laying System

(a)  Single-ply layup of boron-epoxy tape for the horizontal stabilizer for an F-14 fighter aircraft.  (b)  A 10-axis computer-numerical-controlled tape-laying system.  This machine is capable of laying up 75- and 150-mm (3- and 6-in.) wide tapes on contours of up to +/- 30 degrees and at speeds of up to 0.5m/s (1.7 ft/s). Source:  (a)  Courtesy of Grumman Aircraft Corporation.  (b)  Courtesy of The Ingersoll Milling Machine Company.

Production of Fiber-Reinforced Plastic Sheets

Schematic illustration of the manufacturing process for producing fiber-reinforced plastic sheets.  The sheet still is viscous at this stage and later can be shped into various products.  Source:  After T. W. Chou, R. L. McCullough, and R. B. Pipes.

Vacuum-Bag Forming and Pressure-Bag Forming

Schematic illustration of (a) vacuum-bag forming, and (b) pressure-bag forming.  These processes are used in making discrete reinforced plastic parts.  Source:  After T. H. Meister.

Open-Mold Processing

Manual methods of processing reinforced plastics:  (a) hand lay-up, and (b) spray lay-up.  Note that, even though the process is slow, only one mold is required.  The figures show a female mold, but male molds also are used.  These methods also are called open-mold processing.  (c)  A boat hull made by these processes

Filament-Winding

(a)  Schematic illustration of the filament-winding process; (b) fiberglass being wound over aluminum liners for slide-raft  inflation vessels for the Boeing 767 aircraft.  The products made by this process have high strength-to-weight ratio and also serve as lightweight pressure vessels.  Source:  Courtesy of Brunswick Corporation.

Pultrusion

(a)  Schematic illustration of the pultrusion process.  (b)  Examples of parts made by pultrusion.  The major components of fiberglass ladders (used especially by electricians) are made by this process.  Unlike aluminum ladders, they are available in different colors but are heavier because of the presence of glass fibers. Source: Courtesy of Strongwell Corporation.

## Postupci izrade proizvoda s keramičkom matricom

Postupci su izrade proizvoda s keramičkom matricom:

### Toplo prešanje

### Toplo izostatičko prešanje HIP (en. Hot Isostatic Pressing)

### Sinteriranje iz tekuće faze

- Toplo prešanje

In Hot Pressing technique, pressure and temperature are applied simultaneously. Application of pressure at sintering temperature accelerates the kinetics of densification by increasing the contact stress between particles of matrix and particulates/ fibers of dispersed ceramic phase.

- Toplo izostatičko prešanje HIP (en. Hot Isostatic Pressing)

In Hot Isostatic Pressing technique, the ceramic particles of matrix containing particulates/ fibers of dispersed ceramic phase are contained in a rubber envelop and the pressure is applied by a fluid, isostatically (i.e. has the same magnitude in all directions) along with temperature simultaneously.

- Sinteriranje iz tekuće faze

Liquid phase sintering involves the presence of a viscous liquid at sintering temperatures. The liquid in the narrow channels between the particles (reinforcements) results in substantial capillary action, which aids in densification.

## Postupci izrade proizvoda s metalnom matricom

- Better temperature resistance than polymer-matrix composites

- Lower temperature resistance than ceramic-matrix composites

- High fabrication cost compared to polymer-matrix composites

- Low fabrication cost compared to ceramic-matrix composites

### Lijevanje s miješanjem

### Infiltracija

### Depozicija

### Difuzijsko spajanje

### Formiranje s deformacijom

Postupci su izrade proizvoda s metalnom matricom:

- Lijevanje s miješanjem

- Squeeze Infiltration

- Reactive Processing

- Powder Blending & Consolidation

- Fizičko deponiranje pare

- Particle-Liquid Sheet Impingement Technique

- Dvostupanjski process: Two stage process: Quick-Set and Quick-Cast

- Liquid metal infiltration

- Hot pressing above the solidus of the matrix metal

- Powder metallurgy (diffusion bonding)

- Plasma spraying

- Lijevanje s miješanjem

Talina s dodanim krutim česticama keramike se miješa i po homogenizaciji se smjesa ohladi.

- Squeeze Infiltration

Liquid metal is injected into the interstices of an assembly of short fibers, usually called a preform.

- Reactive Processing

Several processes have been developed in which constituents are brought together under conditions such that a chemical reaction occurs while the mixture consolidates.

- Powder Blending & Consolidation

Blending of metallic powder with ceramic fibers or particulate is a versatile technique for MMC production. This is usually followed by cold compaction and a high temperature consolidation stage such as Hot Isostatic Pressing (HIP) or extrusion.

- Fizičko deponiranje pare PVD (en. Physical Vapor Deposition)

This process involves passing the fiber through a region having a high vapor pressure of the metal to be deposited, where condensation takes place so as to produce a thick surface coating. Composite fabrication is completed by assembling the coated fibers into a bundle and consolidating by hot pressing or HIP.

- Particle-Liquid Sheet Impingement Technique

In this technique, ceramic particles are impacted on a thin and flowing sheet of liquid metal. The matrix metal is melted and ejected at a high velocity from a small diameter circular orifice. The liquid jet then impinge on a stationary or spinning circular solid disk made of high temperature ceramic. The ceramic particles are injected onto the liquid metal flow. The liquid metal sheet containing ceramic particles break up into small drops. The composite drops are collected and solidified rapidly. The composite is further compacted by hot press sintering or by hot rolling.

- Dvostupanjski process: Two stage process: Quick-Set and Quick-Cast

The first process Quick-Set produces a porous net shaped ceramic item using a low pressure, low viscosity injection moulding process. This is followed by pressure assisted infiltrations of the ceramic form by molten metal by a process called Quick- Cast.

Aluminum-matrix composite brake caliper using nanocrystallyne alumina fiber reinforcement.  Source:  Courtesy of 3M Corp.

## Procesi izrade i proizvodi od kompozita

### Granične površine faza

### Mehanička svojstva kompozita

### Usporedba postupaka

### Greške i njihovo otklanjanje

## Literatura

- Kolumbić Z., Tomac N.: Materijali – podloge za diskusiju; Sveučilište u Rijeci; Filozofski fakultet, Odsjek za politehniku, Rijeka 2005; http://www.ffri.hr/~zvonimir/.